Appendix:

Effect of V-VIB group ternary elements on the properties of Ti2AlM-type O-phases: A first-principles study

Zeinab Heidari Pebdani1,2*, Florian Pyczak1,2, and Rebecca Janisch3

1Helmholtz Zentrum Hereon, Geesthacht, Germany

2Brandenburgische Technische Universität Cottbus-Senftenberg, Germany

3Interdisciplinary Centre for Advanced Materials Simulation (ICAMS) Ruhr-University Bochum, Germany.

(Dated: June. 26, 2024)

-----------------------

* To whom correspondence should be addressed; Email: zeinab.heidaripebdani@hereon.de

Appendix A.

EforTi2AlM=14EtotalTi2AlM−2EatomTi−EatomAl−EatomM             (1)

C11+C22−2C12>0,C11+C33−2C13>0,C22+C33−2C23>0;Cij>0i∼16, C11+C22+C33+2C12+2C13+2C23>0                                                                                      (2)

BV=19C11+2C12+2C13+C22+2C23+C33,

GV=115C11−C12−C13+C22−C23+C33+3C44+3C55+3C66                                    (3)

BR=XC11C22+C33−2C23+C22C33−2C13−2C33C12+C122C23−C12+C132C12−C13+C232C13−C23−1,

GR=154XC11C22+C33+C23+C22C33+C13+C33C12−C12C23+C12−C13C12+C13−C23C13+C23+3C44−1+C55−1+C66−1,

X=C13C12C23−C13C22+C23C12C13−C23C11+C33C11C22−C122                             (4)

B=BV+BR2,G=GV+GR2                                                                                                          (5)

E=9BG3B+G,ν=3B−2G6B−2G                                                                                                             (6)

HV=2k2G0.583−3                                                                                                               (7)

010} planes, and A {100} in {100} planes are the single crystal shear anisotropy factors that are defined as77.

A100=4C44C11+C33−2C13 , A010=4C55C22+C33−2C23, A001=4C66C11+C22−2C12                             (8)

AB=BV−BRBV+BR,AG=GV−GRGV+GR                                                                                                     (9)

AU=BVBR+5GVGR−6                                                                                                                        (10)

AL=ln⁡BVBR2+5lnGVGR2                                                                                                              (11)

θD=ℎk3n4πNAρM13νm                                                                                                             (12)

νm=132νt3+1νl313                                                                                                                  (13)

νt=Gρ12νl=B+4G3ρ12                                                                                                      (14)

Appendix B.

(a)

(b)

(c)

Fig.S.1. Crystal structure of the O-phase Ti2AlM (M= V, Nb, Ta, Mo, and W) intermetallic compound from three different direction a) [001], b) [010], c) [100]; Wyckoff positions are labeled in the representation in the center.

Fig. S.2. (a) Energy (eV) vs Iteration steps, and (b) Energy (eV) vs. Lattice constant (Å) for Ti (hcp).

Fig.S.3. Calculated energy versus volume (Å3) curves of Ti2AlM O-phases.

Fig.S.4. Convergence chart of the total energy defined in Equation (1) as the function of the number of irreducible k-points. Five representative elements are shown: Kpoint vs. Energy total for (a) Ti2AlV; (b) Ti2AlNb; (c) Ti2AlTa; (d) Ti2AlMo; (e) Ti2AlW crystal structures.

Fig.S.5. Convergence chart of the total energy defined in Equation (1) as the function of the number of irreducible k-points. Summary Energy total  vs. Energy Cutoff of  O-phase (a) Ti2AlV; (b) Ti2AlNb; (c) Ti2AlTa; (d) Ti2AlMo; (e) Ti2AlW crystal structures.

Fig.6.S.  Total energy vs c/a variations of alloys:  a) Ti2AlMo, b) Ti2AlNb.  The symbols denote the calculated energies while the lines show the fitted Murnaghan equation of state (3).

d) M_V

a) M_Nb

b) M_Ta

c) M_Mo

e) M_W

Fig.7.S. Variation of DFT total energy vs lattice constant of alloys: a) Ti2AlV, b) Ti2AlNb, c) Ti2AlTa, d) Ti2AlMo, e) Ti2AlW.  The symbols denote the calculated energies while the lines show the fitted Murnaghan equation of state (3). The minimum energy (eV) corresponds to the Zero-pressure lattice constant (Angstrom).

Table.S. 1. Calculated equilibrium lattice constants a, b, c (A°) and Energy total and formation energy (eV) per atom, and K-mesh and Energy Cut off for o phase Ti2AlM alloys alongside PAW-PBE pseudo-potentials.

| Alloys | Pot | Atoms | a (Å) | b (Å) | c (Å) | c/a (Å) | E_tot/atom | E_for/atom | K-mesh |  |  | En-Cut |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| O-phase | PAW_PBE |  | Calc. | Calc. | Calc. | Calc. | (eV) | (eV) | Kx | Ky | Kz | (eV) |
| Ti2AlV | Ti, V | 16 | 5.8843941272924845 | 9.3372394782140891 | 4.5378384308587316 | 0.757377049 | −7.256925625 | -0.2035905 | 11 | 9 | 7 | 600 |
| Ti2AlMo | Ti, Mo | 16 | 6.1674013277279496 | 9.1982542189344052 | 4.4910511184175448 | 0.728191807 | −7.888863642 | -0.33269775 | 11 | 9 | 7 | 600 |
| Ti2AlTa | Ti, Ta | 16 | 6.0646126009253356 | 9.4623228729721429 | 4.6584297315838130 | 0.768133109 | −8.028395152 | −0.307366451 | 11 | 9 | 7 | 600 |
| Ti2AlW | Ti, W | 16 | 6.1371482820065575 | 9.2324433069801053 | 4.5126365136325797 | 0.735298596 | −8.330823223 | -0.256904 | 11 | 9 | 7 | 600 |
| Ti2AlW | Ti, W_sv | 16 | 6.0179729862251472 | 9.3154614167717700 | 4.5631461434443565 | 0.758253012 | −8.305356804 | -0.247944304 | 11 | 9 | 7 | 600 |
| Ti2AlNb | Ti_pv, Nb_pv | 16 | 6.0633844589243937 | 9.5359655160819283 | 4.6790461841898860 | 0.771688851 | -7.64152125 | -0.2779695 | 11 | 9 | 7 | 600 |
| Ti2AlNb | Ti, Nb_pv | 16 | 6.0489023317249311 | 9.5201257303019151 | 4.6708553047294465 | 0.772182298 | −7,620760607 | -0.2792025 | 11 | 9 | 7 | 600 |

Table.S 2. Calculated equilibrium lattice constants a, b, c (A°) and Energy total and formation energy (eV) per atom, and K-mesh and Energy Cut off for o phase Ti2AlM alloys alongside PAW-GGA pseudo-potentials.

| Alloys | Pot | Atoms | a (Å) | b (Å) | c (Å) | c/a (Å) | E_tot/atom | E_for/atom | K-mesh |  |  | En-Cut |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| O-phase | PAW_GGA |  | Calc. | Calc. | Calc. | Calc. | (eV) | (eV) | Kx | Ky | Kz | (eV) |
| Ti2AlV | Ti, V | 16 | 5.8779937333355416 | 9.3335983470169914 | 4.5377819017936201 | 0.771995022 | −7.228097513 | -0.170359263 | 11 | 9 | 7 | 600 |
| Ti2AlMo | Ti, Mo | 16 | 6.1709713432862099 | 9.1929978759549940 | 4.4864583401528577 | 0.72702628 | −7.86255296 | -0.3074315 | 11 | 9 | 7 | 600 |
| Ti2AlTa | Ti, Ta | 16 | 6.0598036493841780 | 9.4595013286873719 | 4.6617643625649396 | 0.769292973 | −7.988751718 | -0.155274956 | 11 | 9 | 7 | 600 |
| Ti2AlW | Ti, W_pv | 16 | 6.1359669891308393 | 9.2547718755604382 | 4.5198862798934822 | 0.736621675 | −8.264512358 | −0.241074608 | 11 | 9 | 7 | 600 |
| Ti2AlW | Ti, W | 16 | 6.1414231067698282 | 9.2340301004078409 | 4.5096566826901512 | 0.734301579 | −8.292429863 | -0.2352979999 | 11 | 9 | 7 | 600 |
| Ti2AlNb | Ti_pv, Nb_pv | 16 | 6.0595920783240560 | 9.5362621013885249 | 4.6769899530042744 | 0.771832475 | −7.608774375 | −0.280442889 | 11 | 9 | 7 | 600 |
| Ti2AlNb | Ti, Nb_pv | 16 | 6.0451359551952502 | 9.5190192340862563 | 4.6696068262394554 | 0.772456875 | −7.593353125 | −0.251278014 | 11 | 9 | 7 | 600 |

(a)

(b)

(c)

(d)

Fig.8.S. Ti2AlM O-phases: a) Energy of formation using the GGA and PBE pseudopotentials for V, Nb, Ta, Mo, and W. b) The c/b variation for PAW-PBE and PAW-GGA. c) The a/b variation for PAW-PBE and PAW-GGA. d) The c/a variation for PAW-PBE and PAW-GGA (for M pvpseudopotentials, the semi core p states are treated as valence.For M sv pseudopotentials, the semi core s states are treated as valence).

Table 3.S. Calculated elastic constants Cij for the O-phase Ti2AlM (M= V, Nb, Ta, Mo, and W) at 0 K. All values are in GPa.

| Alloys | C11 | C12 | C13 | C23 | C33 | C22 | C44 | C55 | C66 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ti2AlV | 160.172 | 70.281 | 64.375 | 60.375 | 190.562 | 160.827 | 60.729 | 61.271 | 65.619 |
| Ti2AlNb | 163.056 | 71.215 | 79.048 | 60.048 | 200.846 | 195.958 | 51.632 | 54.743 | 62.992 |
| Ti2AlTa | 187.788 | 75.181 | 91.799 | 42.599 | 246.522 | 159.009 | 52.723 | 50.996 | 79.836 |
| Ti2AlMo | 178.873 | 86.006 | 117.165 | 70.165 | 245.875 | 218.790 | 79.000 | 51.109 | 30.980 |
| Ti2AlW | 191.000 | 74.011 | 114.908 | 50.908 | 248.006 | 206.000 | 49.579 | 48.132 | 79.013 |

Table 4.S. Calculated Bulk modulus (B), Young’s Modulus (E), Poisson’s ratio (ν), Shear modulus (G), Pugh’s ratio (k), using Reuss (R), Voigt (V), for the O-phase Ti2AlM (M= V, Nb, Ta, Mo, and W) compounds, and their related mechanical constants (B/G, k, ΘD), Hardness Hv, and Anisotropic properties AG, AU , AL at 0 Kelvin.  B, E, ν, G, k, Hv, and AG, AU , AL are in GPa and ΘD in Kelvin.

| Alloys | B | E | ν | G | B/G | k | Hv | AG | AU | AL | ΘD |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ti2AlV | 96.232 | 138.595 | 0.382 | 55 | 1.75 | 0.572 | 7.846 | 0.71 | 0.07 | 0.03 | 416 |
| Ti2AlNb | 108.383 | 143.317 | 0.396 | 56 | 1.93 | 0.516 | 6.717 | 1.13 | 0.12 | 0.05 | 422 |
| Ti2AlTa | 110.973 | 141.606 | 0.401 | 55 | 2.02 | 0.495 | 6.158 | 4.38 | 0.50 | 0.20 | 389 |
| Ti2AlMo | 131.354 | 135.467 | 0.425 | 51 | 2.57 | 0.388 | 3.590 | 1.13 | 0.12 | 0.05 | 333 |
| Ti2AlW | 124.352 | 143.800 | 0.414 | 55 | 2.25 | 0.442 | 5.022 | 3.18 | 0.35 | 0.14 | 349 |

(Ⅰ)

(Ⅱ)

(Ⅲ)

(Ⅳ)

Fig.9.S. The 3D illustration of Ⅰ) Young’s modulus, Ⅱ) Shear modulus, Ⅲ) Isotropic Linear compressibility, and Ⅳ) Poisson’s ratio of corresponding stiffness for the O-phase Ti2AlMo. All values are in GPa.

Fig.10.S. Projections of a) Bulk Modulus, b) Shear Modulus, and c) Young’s Modulus on [010] direction for Ti2AlM O-phases.

Fig. S.11. Total and partial density of states (DOSs) of (a) Ti2AlV (b) Ti2AlNb (c) Ti2AlTa (d) Ti2AlMo (f) Ti2AlW O-phase.

Fig. S. 12. Band structures and density of states (DOSs) of (a) Ti2AlV (b) Ti2AlNb (c) Ti2AlTa (d) Ti2AlW (f) Ti2AlMo O-phase prismatic plane.

Table.S. I- Summary of pure metal parameters calculated values via PAW-PBE method.

| Alloys | Pot | Atoms | a (Å) | b (Å) | c (Å) | c/a (Å) | E_tot | E_tot/atom | K-mesh |  |  | En-Cut |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Phase | PAW_PBE |  | Calc. | Calc. | Calc. | Calc. | (eV) | (eV) | Kx | Ky | Kz | (eV) |
| Ti (hcp) | Ti_pv | 2 | 2.9358502048699 | 2.9358502048699 | 4.65614488652455 | 1.585 | -15.612339 | -7.8061695 | 12 | 12 | 8 | 520 |
| Ti (hcp) | Ti | 2 | 2.9184206990000 | 2.9358502048699 | 4.6204905820000 | 1.585 | -15.52436815 | −7.762184075 | 12 | 12 | 8 | 520 |
| Al (fcc) | Al | 4 | 4.04188141438616 | 4.04188141438616 | 4.04188141438616 | 1 | -14.995458 | -3.748865 | 12 | 12 | 12 | 500 |
| Nb (bcc) | Nb_pv | 2 | 3.3218819737153917 | 3.3218819737153917 | 3.3218819737153917 | 1 | -20.186001 | -10.093005 | 11 | 11 | 11 | 550 |
| Mo (bcc) | Mo_pv | 2 | 3.15909603636958 | 3.15909603636958 | 3.15909603636958 | 1 | -21.86009 | -10.930045 | 12 | 12 | 12 | 550 |
| Mo (bcc) | Mo | 2 | 3.1510668383380809 | 3.1510668383380809 | 3.1510668383380809 | 1 | -21.90286491 | −10.951432455 | 12 | 12 | 12 | 550 |
| V (bcc) | V | 2 | 2.9794000000000000 | 2.9794000000000000 | 2.9794000000000000 | 1 | -17.88021854 | −8.94010927 | 14 | 14 | 14 | 500 |
| V (bcc) | V_pv | 2 | 2.9998000000000000 | 2.9998000000000000 | 2.9998000000000000 | 1 | -17.91252778 | −8.95626389 | 14 | 14 | 14 | 500 |
| Ta (bcc) | Ta_pv | 4 | 4.22413560297557 | 4.22413560297557 | 4.22413560297557 | 1 | -46.297228 | -11.574307 | 14 | 14 | 14 | 500 |
| Ta (bcc) | Ta | 4 | 4.2267999999999999 | 4.2267999999999999 | 4.2267999999999999 | 1 | -46.44243679 | −11.610609198 | 14 | 14 | 14 | 500 |
| W(bcc) | W_sv | 2 | 3.1907000000000001 | 3.1907000000000001 | 3.1907000000000001 | 1 | -25.9128342 | -12.956417 | 14 | 14 | 14 | 500 |
| W (bcc) | W | 2 | 3.1720999999999999 | 3.1720999999999999 | 3.1720999999999999 | 1 | -26.0448862 | −13.0224431 | 14 | 14 | 14 | 500 |

Table.S.II- Summary of pure metal parameters calculated values via PAW-GGA method.

| Alloys | Pot | Atoms | a (Å) | b (Å) | c (Å) | c/a (Å) | E_tot | E_tot/atom | K-mesh |  |  | En-Cut |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Phase | PAW_GGA |  | Calc. | Calc. | Calc. | Calc. | (eV) | (eV) | Kx | Ky | Kz | (eV) |
| Ti (hcp) | Ti_pv | 2 | 2.93097225700000 | 2.93097225700000 | 2.93097225700000 | 1.585 | -15.54872300 | −7.7743615 | 12 | 12 | 8 | 520 |
| Ti (hcp) | Ti | 2 | 2.9338138103000002 | 2.9338138103000002 | 4.6570091248000001 | 1.585 | -15.60370000 | −7.80185000 | 12 | 12 | 8 | 520 |
| Al (fcc) | Al | 4 | 4.0437000000000003 | 4.0437000000000003 | 4.0437000000000003 | 1 | -14.80623101 | -3.701558 | 12 | 12 | 12 | 500 |
| Nb (bcc) | Nb_pv | 2 | 3.3240841764021911 | 3.3240841764021911 | 3.3240841764021911 | 1 | -20.12608489 | −10.063042445 | 11 | 11 | 11 | 550 |
| Mo (bcc) | Mo | 2 | 3.1587999999999998 | 3.1587999999999998 | 3.1587999999999998 | 1 | -21.83045611 | −10.915228055 | 12 | 12 | 12 | 550 |
| V (bcc) | V | 2 | 2.97733270970201 | 2.97733270970201 | 2.97733270970201 | 1 | -17.851389 | -8.9256945 | 14 | 14 | 14 | 500 |
| Ta (bcc) | Ta | 4 | 4.2267999999999999 | 4.2267999999999999 | 4.2267999999999999 | 1 | −46.0954167 | −11,523854175 | 14 | 14 | 14 | 500 |
| W(bcc) | W_pv | 2 | 3.1907000000000001 | 3.1907000000000001 | 3.1907000000000001 | 1 | -25.57698641 | −12.788493205 | 14 | 14 | 14 | 500 |
| W (bcc) | W | 2 | 3.1720999999999999 | 3.1720999999999999 | 3.1720999999999999 | 1 | -25.84653941 | −12,923269705 | 14 | 14 | 14 | 500 |

Appendix. Supplementary data

Supplementary material related to this article can be found online deposited at  https://doi.org/10.5281/zenodo.7687784 .

Appendix C.

All POSCAR files listed below are available for further consideration.

#POSCAR files

#O-Phase Ti2AlV

1.0

6.100000 0.000000 0.000000

0.000000 9.570000 0.000000

0.000000 0.000000 4.620000

Ti Al V

8 4 4

direct

0.231000  0.904000 0.250000 Ti

-0.231000  0.904000 0.250000 Ti

0.731000  1.404000 0.250000 Ti

0.269000  1.404000 0.250000 Ti

-0.231000 -0.904000 0.750000 Ti

0.231000 -0.904000 0.750000 Ti

0.269000 -0.404000 0.750000 Ti

0.731000 -0.404000 0.750000 Ti

0.000000  0.163000 0.250000 Al

0.000000 -0.163000 0.750000 Al

0.500000  0.663000 0.250000 Al

0.500000  0.337000 0.750000 Al

0.000000  0.636000 0.250000 V

0.000000 -0.636000 0.750000 V

0.500000  1.136000 0.250000 V

0.500000 -0.136000 0.750000 V

==========================

#O-Phase Ti2AlNb

1.0

6.100000 0.000000 0.000000

0.000000 9.570000 0.000000

0.000000 0.000000 4.620000

Ti Al Nb

8 4 4

direct

0.231000  0.904000 0.250000 Ti

-0.231000  0.904000 0.250000 Ti

0.731000  1.404000 0.250000 Ti

0.269000  1.404000 0.250000 Ti

-0.231000 -0.904000 0.750000 Ti

0.231000 -0.904000 0.750000 Ti

0.269000 -0.404000 0.750000 Ti

0.731000 -0.404000 0.750000 Ti

0.000000  0.163000 0.250000 Al

0.000000 -0.163000 0.750000 Al

0.500000  0.663000 0.250000 Al

0.500000  0.337000 0.750000 Al

0.000000  0.636000 0.250000 Nb

0.000000 -0.636000 0.750000 Nb

0.500000  1.136000 0.250000 Nb

0.500000 -0.136000 0.750000 Nb

=========================

#O-Phase Ti2AlTa

1.0

6.100000 0.000000 0.000000

0.000000 9.570000 0.000000

0.000000 0.000000 4.620000

Ti Al Ta

8 4 4

direct

0.231000  0.904000 0.250000 Ti

-0.231000  0.904000 0.250000 Ti

0.731000  1.404000 0.250000 Ti

0.269000  1.404000 0.250000 Ti

-0.231000 -0.904000 0.750000 Ti

0.231000 -0.904000 0.750000 Ti

0.269000 -0.404000 0.750000 Ti

0.731000 -0.404000 0.750000 Ti

0.000000  0.163000 0.250000 Al

0.000000 -0.163000 0.750000 Al

0.500000  0.663000 0.250000 Al

0.500000  0.337000 0.750000 Al

0.000000  0.636000 0.250000 Ta

0.000000 -0.636000 0.750000 Ta

0.500000  1.136000 0.250000 Ta

0.500000 -0.136000 0.750000 Ta

==========================

#O-Phase Ti2AlMo

1.0

6.100000 0.000000 0.000000

0.000000 9.570000 0.000000

0.000000 0.000000 4.620000

Ti Al Mo

8 4 4

direct

0.231000  0.904000 0.250000 Ti

-0.231000  0.904000 0.250000 Ti

0.731000  1.404000 0.250000 Ti

0.269000  1.404000 0.250000 Ti

-0.231000 -0.904000 0.750000 Ti

0.231000 -0.904000 0.750000 Ti

0.269000 -0.404000 0.750000 Ti

0.731000 -0.404000 0.750000 Ti

0.000000  0.163000 0.250000 Al

0.000000 -0.163000 0.750000 Al

0.500000  0.663000 0.250000 Al

0.500000  0.337000 0.750000 Al

0.000000  0.636000 0.250000 Mo

0.000000 -0.636000 0.750000 Mo

0.500000  1.136000 0.250000 Mo

0.500000 -0.136000 0.750000 Mo

=============================

#O-Phase Ti2AlW

1.0

6.100000 0.000000 0.000000

0.000000 9.570000 0.000000

0.000000 0.000000 4.620000

Ti Al W

8 4 4

direct

0.231000  0.904000 0.250000 Ti

-0.231000  0.904000 0.250000 Ti

0.731000  1.404000 0.250000 Ti

0.269000  1.404000 0.250000 Ti

-0.231000 -0.904000 0.750000 Ti

0.231000 -0.904000 0.750000 Ti

0.269000 -0.404000 0.750000 Ti

0.731000 -0.404000 0.750000 Ti

0.000000  0.163000 0.250000 Al

0.000000 -0.163000 0.750000 Al

0.500000  0.663000 0.250000 Al

0.500000  0.337000 0.750000 Al

0.000000  0.636000 0.250000 W

0.000000 -0.636000 0.750000 W

0.500000  1.136000 0.250000 W

0.500000 -0.136000 0.750000 W

================================